Snowmass 2021 Letter of Interest

### Fabrication of 1.3 GHz ILC Shaped Magnesium Diboride SRF Cavity

Primary Contact: Xiaoxing Xi

Temple University, Philadelphia, PA 19122, USA

xiaoxing@temple.edu

Fay Hannon and Robert Rimmer

Thomas Jefferson National Accelerator Facility, Newport News, Virginia 23606, USA

Alireza Nassiri

Argonne National Laboratory, Argonne, Illinois 60439, USA

Magnesium diboride (MgB2) is a potential higher Tc superconducting material for SRF cavities. Compared to Nb, MgB2 potentially has a lower BCS surface resistance because of the higher transition temperature of 39 K and small normal resistivity [1] and a higher thermodynamic critical field Hc [2, 3]. These properties promise high Q and high accelerating field in SRF cavities.

At Temple University, my group has used the hybrid physical-chemical vapor deposition (HPCVD) technique to deposit high quality MgB2 thin films [4]. We have also used HPCVD to coat the inside wall of 6-GHz stainless steel and niobium cavities [5], 3.9-GHz mock niobium cavities [6], as well as 3-GHz Cu cavity [7]. The Cu cavity offers the advantage of potential high cavity operating temperature at 20 – 25 K due to the high thermal conductivity of Cu. Our previous MgB2 film fabrication on Cu disks and Cu tubes demonstrated coatings with good superconducting properties [8, 9]. These investigations demonstrated the ability of the HPCVD technique to conformally coat curved surfaces such as the inside wall of SRF cavities with superconducting MgB2 layers.

The single-cell 3-GHz MgB2 coated Cu cavity was characterized at JLab. The loaded factor Q as a function of temperature showed a superconducting transition at around 36 K. The Q value and the breakdown field when the MgB2 coating was in the superconducting state, however, were both very low. The poor performance was attributed to the significant existence of the Mg-Cu alloy regions, which are not superconducting in the MgB2 coating. The existence of these regions was due to the insufficient reaction of boron with Mg during the deposition due to the short deposition time, which was limited due to technical difficulties arising from the small size of the 3-GHz cavity. Unfortunately, the work has stopped due to the end of funding

A straightforward improvement of the result on the single-cell 3-GHz Cu cavity could be increasing the deposition time. This, however, is impractical in the current setup due to the small cavity size: Mg vapor condenses on the water-cooled gas line, which drops onto the cavity surface. This problem can be alleviated in a larger coating system, for example, for 1.3-GHz cavities. Thus, with adequate funding, we will build a larger system capable of coating 1.3 GHz ILC shaped SRF cavities. The larger cavity size will help to avoid the Mg condensate from dropping on the cavity surface and allow a larger Mg source for longer deposition to produce continuous and thick MgB2 coating with good RF superconducting properties.

References

[1] Anne-Marie Valente-Feliciano, Superconducting RF materials other than bulk niobium: a review, Supercond. Sci. Technol. 29, 113002 (2016).

[2] F. Bouquet, R. A. Fisher, N. E. Phillips, D. G. Hinks, and J. D. Jorgensen, Specific heat of Mg11B2: evidence for a second energy gap, Phys. Rev. Lett. 87, 047001 (2001).

[3] M. Zehetmayer, M. Eisterer, J. Jun, S. M. Kazakov, J. Karpinski, A. Wisniewski, and H. W. Weber, Mixed-state properties of superconductingMgB2 single crystals, Phys. Rev. B 66, 052505 (2002).

[4] X. X. Xi, MgB2 thin films, Supercond. Sci. Technol. 22, 043001 (2009).

[5] M. A. Wolak, T. Tan, A. Krick, E. Johnson, M. Hambe, Ke Chen and X. X. Xi, Superconducting magnesium diboride coatings for radio frequency cavities fabricated by hybrid physical-chemical vapor deposition, Phys. Rev. ST Accel. Beams 17, 012001 (2014).

[6] Namhoon Lee, W. K. Withanage, T. Tan, M. A. Wolak, A. Nassiri, and X. X. Xi, Hybrid Physical Chemical Vapor Deposition of Magnesium Diboride Inside 3.9 GHz Mock Cavities, IEEE Tran. On Appl. Supercond. 27, 3500304 (2017).

[7] Xin Guo, Wenura K. Withanage, Jay R. Paudel, Grigory Eremeev, Fay Hannon, Robert Rimmer, Alireza Nassiri, Xiaoxing Xi, Fabrication and Radio Frequency Properties of 3-GHz SRF Cavities Coated with MgB2, J. Supercond. & Novel Magnetism, in press.

[8] Wenura K. Withanage, X. X. Xi, Alireza Nassiri, Namhoon Lee et al., ﻿Growth of magnesium diboride films on 2 inch diameter copper discs by hybrid physical–chemical vapor deposition, ﻿Supercond. Sci. Technol. 30, 045001 (2017).

[9] Wenura K. Withanage, ﻿N. H. Lee, Sashank V. Penmatsa, M. A. Wolak, A. Nassiri and X. X. Xi, Magnesium diboride on inner wall of copper tube: A test case for superconducting radio frequency cavities, ﻿Phys. Rev. Accel. Beams 20, 102002 (2017).